L20 DOORS / SHUTTERS / HATCHES

480 STEEL DOORSETS

HINGED SECURITY DOORSETS (HSD)

- MANUFACTURER

ASSA Abloy / BL Shutters Ltd, Carn Rd, Carn Industrial Estate, Portadown, Co Armagh.

Telephone: 028 38333551. Fax: 028 38350204.

Email: sales@blshutters.co.uk . Website: www.blshutters.co.uk

- APPLICATION

WAREHOUSING, FACTORIES, COMMERCIAL BUILDINGS

BL Hinged doors have been designed for a wide range of buildings all manufactured to client
specifications. They require little or no maintenance but provide strength and durability, can be 
used in all applications as timber doors but giving greater security. All doors come complete
with a wide range of hardware. Available in coloured polyester powder coating or primed finish for site painting.

- SIZE

Maximum Size recommended single 1200mm x 3000mm / double 2300mm x 3000mm.

- FIXING

Opening / reveal fixed.

- DOOR LEAF

• Two skins of 1.2mm (18 ga) thick galvanised steel.
• 45mm thick door leaf with no face seams.
• Doors are stiffened, insulated and sound deadened with pre-expanded, small cell honeycomb core 
material and laminated under pressure to face the skins.
• Doors are complete with lock and hardware reinforcements.
• Face skins are connected by a continuous “deep pocket” interlocking edge lock seam for added 
strength and durability.
• 1.6mm (16ga.) steel end channels projection welded to the top and bottom of the door.
• Door edges are bevelled for ease of operation and close fit.
• Doors are morticed, reinforced, drilled and tapped for three templated hinges.
• On double doors, an astragal is fitted to the leading edge of one leaf to ensure a totally sealed unit.

- FIRE RATED

- Can be Fire rated on request, ½ hour to 4 hour

- DOOR FRAME & FIXING

• Manufactured from 1.5mm (16ga.) galvanised steel to BS 1245 with double rebate profile.
• Supplied in either knock down or fully welded smooth finish.
• Corners have integral reinforcements for solid and easy bolting of jambs and head.
• Frames are morticed, reinforced, drilled and tapped for hinges and strikes.
• Hinge and strike reinforcements are protected by metal guard boxes.
• Frames are provided with four fixings per jamb and built-in adjustment and complete over caps.

- TYPICAL HARDWARE

• Assa 3065 sashlock.
• Assa 640 lever handles, cylinder and thumbturn.
• Dorma TS 71 or TS 83 door closer.
• 1.5 pairs of 114mm x 102mm template drilled stainless steel hinges.
• On double doors, 2 lever action flush bolts are located within the 
leading edge of the inactive door leaf.
• A large number of alternative lock and handle arrangements can be 
provided to suit the individual client’s requirements.
• All hardware is factory fitted unless otherwise stated.
The use of BL Shutters approved hardware is strongly recommended since the choice of            hardware can greatly effect fire performance and maintenance.

- FINISH

All doors and frames are manufactured from hot dipped galvanised steel and primed, ready for site 
painting by others or polyester powder coated to choice of colours.

- INSULATION

Optional Rockwool core offering a U-value of 1.41 w/m2k